# Q355 Steel: Q355B Q355C Q355D Properties & Equivalent

CHINESE GB STANDARD

By World Material

ShareFacebookTwitterReddItPinterestEmailLinkedinTumblrTelegram

## Q355 Steel: Q355B, Q355C, Q355D

Q355 steel is a low alloy high strength structural steel commonly used in China, which replaced Q345. The material has a minimum yield strength of 355 MPa (51 ksi) and a tensile strength of 470-630 Mpa (68-91 ksi). According to GB/T 1591 -2018, Q355 has 3 steel grades: Q355AR, Q355M and Q355N, and these steel grades are indicated by the suffix letters B, C, D, E, F for quality grades.

Q355: Q355B, Q355C and Q355D.

Q355M: Q355MB, Q355MC, Q355MD, Q355ME, Q355MF

Q355N: Q355NB, Q355NC, Q355ND, Q355NE, Q355NF

### Meaning (Designation)

- “Q” is the abbreviation of Chinese Pinyin: “Qufu”, which means Yield Strength;

- “355” indicates the minimum yield strength 355 MPa for steel diameter or thickness ≤16mm;

- “AR” refers to As-Rolled, the symbol can be omitted/removed when the delivery condition is hot rolled;

- “M” means Thermomechanically rolled;

- “N” means Normalized or normalized rolled;

- B, C, D, E and F indicate quality grades.

Note: AR, M and N refers to the delivery conditions.

## Q355 Steel Properties

The tables below show Q355 material properties, datasheet and specifications such as chemical composition, and physical and mechanical properties.

### Chemical Composition (Hot rolled)

Hot rolled steel chemical composition based on heat analysis.

| Chemical Composition (Heat Analysis), %, ≤ |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Steel Grade | Quality Grade | C | Si | Mn | P | S | Cr | Ni | Cu | N |
| Q355 | Q355B | 0.24 | 0.55 | 1.6 | 0.035 | 0.035 | 0.30 | 0.30 | 0.40 | 0.012 |
|  | Q355C | 0.20 |  |  | 0.030 | 0.030 |  |  |  | 0.012 |
|  | Q355D | 0.20 |  |  | 0.025 | 0.025 |  |  |  | – |

Note: For quality grades C & D, Carbon content (C)-

- C ≤0.20% when thickness/diameter ≤40mm (1.57 in.);

- C ≤0.22 when thickness/dia. >40mm (1.57 in.);

Normalized or normalized rolled steel

| Chemical Composition (Heat Analysis), % |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Steel Grade | Quality Grade | C, ≤ | Si, ≤ | Mn | P, ≤ | S, ≤ | Cr, ≤ | Ni, ≤ | Cu, ≤ | Mo, ≤ | N, ≤ | Nb | V | Ti | Al, ≥ |
| Q355N | Q355NB | 0.20 | 0.5 | 0.90-1.65 | 0.035 | 0.035 | 0.30 | 0.50 | 0.40 | 0.10 | 0.015 | 0.005-0.05 | 0.01-0.12 | 0.006-0.05 | 0.015 |
|  | Q355NC | 0.20 |  |  | 0.030 | 0.030 |  |  |  |  |  |  |  |  |  |
|  | Q355ND | 0.20 |  |  | 0.030 | 0.025 |  |  |  |  |  |  |  |  |  |
|  | Q355NE | 0.18 |  |  | 0.025 | 0.020 |  |  |  |  |  |  |  |  |  |
|  | Q355NF | 0.16 |  |  | 0.020 | 0.010 |  |  |  |  |  |  |  |  |  |

Thermomechanically rolled steel

| Chemical Composition (Heat Analysis), % |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Steel Grade | Quality Grade | C, ≤ | Si, ≤ | Mn, ≤ | P, ≤ | S, ≤ | Cr, ≤ | Ni, ≤ | Cu, ≤ | Mo, ≤ | N, ≤ | Nb | V | Ti | Al, ≥ |
| Q355M | Q355MB | 0.14 | 0.5 | 1.60 | 0.035 | 0.035 | 0.30 | 0.50 | 0.40 | 0.10 | 0.015 | 0.01-0.05 | 0.01-0.10 | 0.006-0.05 | 0.015 |
|  | Q355MC |  |  |  | 0.030 | 0.030 |  |  |  |  |  |  |  |  |  |
|  | Q355MD |  |  |  | 0.030 | 0.025 |  |  |  |  |  |  |  |  |  |
|  | Q355ME |  |  |  | 0.025 | 0.020 |  |  |  |  |  |  |  |  |  |
|  | Q355MF |  |  |  | 0.020 | 0.010 |  |  |  |  |  |  |  |  |  |

Notes:

- For bars and sections, the P and S content can be 0.005% higher.

- For Ti content, can be up to 0.20%.

### Carbon Equivalent (CEV)

Based on smelting analysis, steel delivered in hot rolled state.

|  |  | CEV (Mass fraction ≤%); Nominal thickness or diameter (d) |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| Steel Grade | Quality Grade | ≤ 30 | 30 < d ≤ 63 | 63 < d ≤ 150 | 150 < d ≤ 250 | 250 < d ≤ 400 |
| Q355 | Q355B | 0.45 (CEV) | 0.47 | 0.47 | 0.49 | – |
|  | Q355C |  |  |  |  | – |
|  | Q355D |  |  |  |  | 0.49 |

### Q355 Material Mechanical Properties

### Notes:1 MPa = 1 N/mm2

### 1 GPa = 1 kN/mm2

Q355 steel mechanical properties are listed in the data sheet below, including yield strength, tensile strength and elongation, etc.

#### Yield Strength

| Yield Strength (≥ MPa), Thickness or Dia. (d) mm |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Steel Grade | Quality Grade |  | d≤16 | 16< d ≤40 |  | 40 < d ≤63 |  | 63 < d ≤ 80 |  | 80< d ≤ 100 | 100< d≤ 150 |  | 150 < d≤ 200 |  | 200 < d ≤ 250 |  | 250 < d ≤ 400 |
| Q355 | Q355B |  | 355 | 345 |  | 335 |  | 325 |  | 315 | 295 |  | 285 |  | 275 |  | – |
|  | Q355C |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | – |
|  | Q355D |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 265 |
| Q355N | All |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | – |
| Yield Strength (≥ MPa), Thickness or Dia. (d) mm |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Steel Grade |  | Quality Grade |  |  | d≤16 |  | 16< d ≤40 |  | 40 < d ≤63 |  |  | 63 < d ≤ 80 |  | 80< d ≤ 100 |  | 100< d≤ 120 |  |
| Q355M |  | All |  |  | 355 |  | 345 |  | 335 |  |  | 325 |  | 325 |  | 320 |  |

#### Tensile Strength

| Tensile Strength, MPa; Dia. (d) mm |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Steel Grade | Quality Grade | d≤100 |  | 100< d ≤250 | 250< d ≤400 |
| Q355 | Q355B | 470-630 |  | 450-600 | – |
|  | Q355C |  |  |  | – |
|  | Q355D |  |  |  | 450-600 |
| Q355N | All |  |  |  | – |
| Tensile Strength, MPa; Dia. (d) mm |  |  |  |  |  |
| Steel Grade | Quality Grade | d≤40 | 40< d ≤63 | 63< d ≤100 | 100< d ≤120 |
| Q355M | All | 470-630 | 450-610 | 440-600 | 430-590 |

#### Elongation

| Elongation (%); Dia. (d) mm; (Hot rolled) |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| Sample direction | d≤40 | 40< d ≤63 | 63< d ≤100 | 100< d ≤150 | 150< d≤ 200 | 250< d ≤400 |
| Transverse | 20 | 19 | 18 | 18 | 17 | 17 |
| Vertical | 22 | 21 | 20 | 18 | 17 | 17 |

#### Charpy Impact

Charpy (V-notch) impact test temperature and impact absorption energy (KV2/J).

| Quality Grade | Temperature, °C (°F) | Longitudinal Impact Energy (J), ≥ | Transverse Impact Energy (J), ≥ |
| --- | --- | --- | --- |
| Q355B, Q355MB, Q355NB | 20 (68) | 34 | 27 |
| Q355C, Q355MC, Q355NC | 0 (32) | 34 | 27 |
| Q355D | -20 (-4) | 34 (Only for thickness ≥250mm) | 27 (for thickness ≥250mm) |
| Q355ND, Q355MD | 20 (68) | 55 | 31 |
|  | 0 (32) | 47 | 27 |
|  | -20 (-4) | 40 | 20 |
| Q355NE, Q355ME | 20 (68) | 63 | 40 |
|  | 0 (32) | 55 | 34 |
|  | -20 (-4) | 47 | 27 |
|  | -40 (-40) | 31 | 20 |
| Q355NF, Q355MF | 20 (68) | 63 | 40 |
|  | 0 (32) | 55 | 34 |
|  | -20 (-4) | 47 | 27 |
|  | -40 (-40) | 31 | 20 |
|  | -60 (-76) | 27 | 16 |

### Physical Properties

Density: 7850 kg/m3 (0.284 lb/in3)

Melting point: 1450-1530 °C (2640-2800 °F)

## Features and Applications

Q355 steel has good mechanical properties, good weldability, hot and cold processing properties and corrosion resistance. Can be used to manufacture ships, boilers, pressure vessels, petroleum storage tanks, bridges, power station equipment, lifting transport machinery and other higher load welded structural parts.

## Q355 Steel Equivalent Grade

Q355 carbon steel equivalent material is listed in the table below including European EN standard (German DIN EN, British BSI, French NF…), ISO, Canada CSA (Canadian Standards Association), Australian/New Zealand and Indian IS standard.

| China |  | ISO |  | European Union |  | Canada |  | Australian/New Zealand |  | Indian |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Standard | Grade | Standard | Grade | Standard | Grade (Material Number) | Standard | Grade – SI (Imperial) | Standard | Grade | Standard | Grade |
| GB/T 1591 -2018 | Q355B | ISO 630-2 | S355B | EN 10025-2 | S355, S355JR (1.0045) | CSA G40.20-13/G40.21-13 | 350W (50W); 345WM (50WM) | AS/NZS 3679.1 | Grade 350; 350L0; 350L15 | IS 2062 | E350 (Fe 490) |
|  | Q355C |  | S355C |  | S355J0 (1.0553) |  |  |  |  |  |  |
|  | Q355D |  | S355D |  | S355J2 (1.0577) |  |  |  |  |  |  |

Related materials: Q235 Material (Q235A, Q235B, Q235C, Q235D) | S235JR (1.0038) | St52-3 Material (1.0570) | S235JRG2 | S235J0 (1.0114) | 1.0117 (S235J2) | S235JRC (EN 1.0122) | St37-2 (1.0037)